

SPECIFICATION & SCHEDULE OF WORKS

32-34 GLOUCESTER STREET, MALMESBURY, SN16 0AA



1) Scaffold rear and side return of building and protect upper decking / paving below with Correx protection sheets.

2) Set up works area in rear courtyard again covering the existing paving with Correx protection sheeting ready for material / waste storage and Hydraulic Lime mixing.

3) Carefully hack off existing Portland cement render back to stone / brick materials underneath and safely remove waste from site. 
Power tools should be avoided to protect historic fabric although may be necessary on the 20th Century rear extension where site poured concrete has been used for the flat roof.

4) Apply dubbing / base coat in 3.5 Hydraulic lime, mixed with a suitable sand at a ratio of 2 sand 1 lime by volume mix - haired with natural horse hair. 

5) Top render coat to the same specification applied and levelled. A stiff brush is used to give a light key. 

6) Two dashing coats applied by hand with a Harling trowel. The mix for this is 4 pea gravel 2 sand 3 hydraulic lime. 

7) The surfaces will then be lime washed with Yellow Ochre pigmented lime wash.

8) Remove scaffolding and clear site.



